## Slide 1: Magnetometry based on defects in isotopically pure silicon carbide
DISTRIBUTION STATEMENT A: Approved for public release, distribution is unlimited.
Allan Bracker, Ignas Lekavicius, S. Carter, S. White2, D. Pennachio1, A. Yeats1, J. Hajzus3, A. Purdy1, T. Reinecke1 , E. Glaser1, and R. Myers-Ward1
1US Naval Research Laboratory, Washington, DC 20375, USA
2NRC Research Associate at the US Naval Research Laboratory, Washington, DC 20375, USA
3ASEE Research Associate at the US Naval Research Laboratory, Washington, DC 20375, USA
+Current affiliation: Laboratory for Physical Sciences, College Park, MD, 20740, USA
Quantum for International Workshop, Rome, NY June 25-27, 2024

## Slide 2
Quantum systems in semiconductors
Advantages
Small size & low power.
Leverage semiconductor industry, potential for integration.
Quantum state “engineering” through growth/fabrication.
Challenges
Loss of quantum coherence to environment.
Inhomogeneity: hard to make them identical.
Crystal defects
Epitaxial quantum dots
Colloidal nanocrystals
Defects in 2D materials.
“Artificial atoms”
Confine electrons in the material.
Discrete orbital energy levels.
Light emission and absorption, optical coherent control.
SiC silicon vacancy
InGaAs quantum dot
2D materials: WSe2, BN, etc.
Colloidal nanocrystals

## Slide 3
Silicon Carbide for quantum S&T
SiC quantum-relevant research activities at NRL
Growth of isotopically-pure SiC
Device fabrication: electronic, photonic, acoustic
Sensing, spin control, quantum optics
Theory & Modelling
Advantages
Wafer scale growth & advanced fab
Membrane-substrates for photonic integration
Optical nonlinearity
Doping / electrical control
Silicon Vacancy
atom-like defect
optically active spin qubit
SiC growth reactor
Code 6880
Ring resonator waveguide
Code 5613
Atom-like optical spectrum
SiCoI: Silicon-Carbide-on-Insulator

## Slide 4
Navy interest in magnetic sensing
Magnetic Anomaly Detection (MAD)
Magnetic fields from submarines, unexploded ordnance, underground anomalies, and vehicles
Magnetic Navigation (MagNav)
Earth’s magnetic anomaly field can be used for navigation

## Slide 5
Quantum for magnetometry
State-of-the-art magnetometers are quantum.
Very sensitive < 1 pT/Hz½
Liquid helium
Big, bulky
Limited dynamic range
Very sensitive < 1 pT/Hz½
Cryogen free
Challenging integration
Defects in solid state
High dynamic range
Room temperature
Lowest SWaP
Natural vector magnetometer
Relative ease of integration
Demonstrated sensitivity  1 pT/Hz½
SQUIDs
(superconducting quantum interference devices)
Atomic vapor
Challenge in SiC: Achieving higher sensitivity
Diamond

## Slide 6
Exploit quantum superposition
Quantum superposition
Superposition phase
time
Signal frequency relates to magnetic field.
Superposition coherence is very sensitive to the environment
 Quantum computing is difficult
 Quantum sensing is comparatively easy
Measurement: Optically-detected magnetic resonance
Laser initializes spins
RF magnetic field BRF manipulates the spins
Readout with spin-dependent photoluminescence
SiC
lens
laser
detector
Bstatic
wave-guide
BRF
c-axis

## Slide 7
Preserving quantum coherence
Superposition phase
time
Higher quantum coherence translates to greater sensitivity
Noisy environment
  Nuclear spins in lattice **
  Phonons (crystal vibration)
  Other defects or electrons nearby
Ensemble inhomogeneity
  Crystal environment: strain, electric, magnetic
  Measurement: optical power, RF power, bias field
29Si: 4.7% and 13C: 1.1%
**Natural abundance of spin-containing isotopes in SiC:
 Reduce sources of noise and inhomogeneity that limit coherence

## Slide 8
Isotopically Pure SiC crystal growth at NRL
Isotopically pure silane gas synthesized with solid Si by Chemistry Division
Grow isotopically purified 4H-SiC on n-doped substrates (Electronics S&T Division) Reduce 29Si: 4.7% → 0.01%, 13C: 1.1% → 0.15%
Electron irradiation creates Si-V defects
4H-SiC, commercial n-doped (~500um)
Epitaxial growth(~20um)
e- irradiation, dose = {,
, , } cm-2
SiC growth reactor
Code 6880
Nat. Abund.
29Si Hyperfine
Isopure
SiC Si-Vacancy: Optically-Detected Magnetic Resonance spectra
No 29Si

## Slide 9
Improvements in spin coherence
Ramsey fringes
T2*: 0.4 μs  5.7 µs
Iso-pure SiC: ~10x increase in coherence time (removes nuclear spin effects).
Judicious choice of quantum state transitions: ~10x increase (remove influence of electric field and strain).
Thermal annealing at 600C: ~50% increase. (Reduces inhomogeneous strain from implantation damage).
T2: 4.5 μs  35 µs
Ramsey fringes
PRXQuantum.3.010343

## Slide 10
Magnetometry with SiC spins
Laser spin initialization & optical detection
Helmholtz coil for bias field
Coplanar waveguide couples RF to SiC
Modulated RF source with Lock-in detection
Detect DC magnetic field
  Frequency domain measurement
  4nT/Hz sensitivity
  Calculated shot noise limit 2 nT/Hz
  Time domain measurement
    4.7nT/Hz sensitivity
    Calculated shot noise limit 200 pT/Hz
Detect AC magnetic field
  Sensitivity for 13 MHz, 101 MHz and 965 MHz detection is 16, 17 and 25 nT/Hz. (Widely tunable compared to diamond)
Three test fields
detect phase shift at fixed time
PhysRevApplied.19.044086
>10x improvement in DC magnetic sensitivity
Optically-detected magnetic resonance

## Slide 11
Telecommunication Wavelength SPS
Frequency conversion in SiC
Direct growth of quantum dots & nanocrystals
1550 nm
Wavelength-tunable Single Photon Source
InAs Quantum dot
Brightness
Single photon purity
Indistinguishability
2-photon interference
Spin-photon interface in SiC, Si
Optical Cavity/Waveguide
Photonic crystal
resident electron
spin
NRL semiconductor quantum research

## Slide 12
Sensing strain with quantum dot molecule
Energy fine-tuning for integration / homogeneity
Site-control of single photon emitters
2 mm
Quantum dots
AFM image
Silicon Carbide
Light emission
NRL semiconductor quantum research

## Slide 13
Supported by US Office of Naval Research
Ignas Lekavicius
Rachael Myers-Ward
Sam Carter (currently at LPS)
Sam White (NRC Postdoc)
Daniel Pennachio
Andrew Yeats
Jenifer Hajzus (ISEE Postdoc)
Andrew Purdy
D. Kurt Gaskill (currently at UMd)
Thomas Reinecke
Evan Glaser
SiC quantum team
Notes: Add plug to PR Applied if published by then